## Slide 1
ALICE Inner Tracking System upgrade:
characterization of first chips fabricated in 65 nm
CMOS technology
Antonio Trifirò*
on behalf of the ALICE Collaboration
* Università degli Studi di Messina -
Dipartimento di Scienze Matematiche e Informatiche, Scienze Fisiche e Scienze della Terra
& Istituto Nazionale di Fisica Nucleare - Sez. di Catania
Italy

## Slide 2
2
Introduction
Motivation of Inner Tracking System upgrade
Overview of sensors development
First submissions in silicon
Sensor optimization
Qualification of the technology
Tests with radioactive source
Beam tests
Tests of radiation damage
Outlook

## Slide 3
- Short-lived heavy hadrons (cτ≈100µm)
- Resonances in the di-electron channel
- Clear separation of interaction vertexes
- Drastic reduction of e background
- Improvement of tracking resolution
- Reduction of material budget
ITS2 innermost 3 layers
ITS3 innermost 3 layers
ITS Upgrade
Upgrade
3
See Valerio SARRITZU’s Pres.
Water Cooling

## Slide 4
MAPS (Monolithic Active Pixel Sensors)
ALice PIxel DEtector (ALPIDE) technology: TowerJazz 180 nm (ITS2)
Detector & readout electronics in a single chip
↓
Elimination of hybrid structures
Low Capacitances → Reduction of Power (10-100mW/cm2)
Reduction of Material Budget &
Bending of large area sensors
↓
Thickness <50µm
↓
180 nm (ITS2) → 65nm (ITS3)
4

## Slide 5
ASICs R&D
1° submissions in silicon with
65 nm Imaging Sensor process:
MLR1 (Multi-Layer per Reticle 1)
APTS (Analogue Pixel Test Structure)
STUDY OF DIFFERENT PIXEL DESIGNS
6×6 pixels (central 4×4 read out)
Pitch: 10, 15, 20, 25 μm
2 versions of output buffers
DPTS (Digital Pixel Test Structure)
STUDY THE IN-PIXEL FULL-DIGITAL FRONT END ELECTRONICS
32 × 32 pixels
Pitch: 15 ×15 µm2
Asynchronous digital readout
Time over Threshold information
Time encoded pixel position
CE65 (Circuit Exploratoire 65 nm)
STUDY PIXEL MATRIX UNIFORMITY
64 ×32 pixels with 15 µm pitch
48 ×32 pixels with 25 µm pitch
Analog Rolling shutter readout 10-40 MHz
3 in pixel architectures
5

## Slide 6
Sensor Optimization: 3 Different Types & 4 Splits
Low dose n-type implant
Low dose n-type implant
Improvement: Charge Collection - Radiation Hardness - Charge Sharing
DEPLETED ZONE
DEPLETED ZONE
DEPLETED ZONE
6
deep p-well → Improvement of circuit-sensor isolation; deep n-well → Improvement of depletion
Split 1: default process
Split 2: first deep p-well adjustment to prevent
punch-through
Split 3: first deep p-well adjustment + deep n-well adjustment
Split 4: (opt. proc.) 1° deep p-well adj. + deep n-well adj. + 2° deep p-well adj. against local potential wells

## Slide 7
APTS-SF
(Source Follower):
direct access to front-end amplitude, without signal processing
APTS-OA
(Operational Amplifier):
fast operational amplifier output buffer for better timing
7
APTS (Analogue Pixel Test Structure)

## Slide 8
APTS-SF
55Fe Source measurement
Sensor Optimization: 3 Different Types
8

## Slide 9
Sensor Optimization: 4 Splits
Split 1: default process
Split 2: first deep p-well adjustment to prevent punch-through
Split 3: first deep p-well adjustment + deep n-well adjustment
Split 4: (optimized process) first deep p-well adjustment +
deep n-well adjustment + second deep p-well adjustment against local potential wells
9

## Slide 10
Standard
Modified
With Gap
APTS-SF
Different Pitches
10

## Slide 11
APTS-SF
Beam Test on different Pitches
11

## Slide 12
APTS-SF
Beam Test on different Pitches
12

## Slide 13
APTS-SF
Beam Test &
Radiation Hardness
After Irradiation with
1015 1MeV neq cm-2
13

## Slide 14
APTS-OPAMP EFFICIENCY
14

## Slide 15
APTS-OPAMP TIMING RESOLUTION
15

## Slide 16
DPTS (Digital Pixel Test Structure)
32 × 32 pixels, pitch 15 ×15 µm2; only Mod. With Gap
55Fe Source
measurement
16

## Slide 17
DPTS Performance vs. Power Consumption
Pixel Power ~Ibias
17

## Slide 18
DPTS
Beam Test &
Radiation Hardness
After Irradiation with
1015 1MeV neq cm-2
18

## Slide 19
DPTS
Beam Test
&
Radiation Hardness
After Irradiation
Not Irradiated
19

## Slide 20
DPTS Source Measurement& Radiation Hardness
20

## Slide 21
APTS – DPTS – CE65 comparison
Beam Test
21

## Slide 22
Conclusions
Different doping profiles, in-pixel electronics architectures and readout flavours implemented
Sensor optimization also proven in 65 nm technology;
Technology qualified and ready for next steps
Engineering Run 1 (ER1) directed to
large, stitched sensor chips
(See V. Sarritzu’s presentation)
Bent Monolithic Active Pixel Sensors
(See D. Colella’s presentation)
22

## Slide 23
SPARE

## Slide 24
Innermost Layer
Innermost Layer
Reduction of Material Budget
24
Azimuthal angle [°]
X/X0 [%] for tracks in |η|<1
Azimuthal angle [°]
X/X0 [%] for tracks in |η|<1

## Slide 25
Improvement of Tracking
FMCT (Fast MonteCarlo Tool) simulations
25

## Slide 26
DPTS Spatial resolution
Spatial Residuals

## Slide 27
Reduction of the beam pipe:
Radius and thickness from
(18.2 mm, 800μm) to (16 mm, 500μm)
Truly cylindrical, wafer-scale sensor: R= 18, 24, 30 mm; L=28 cm
Removal of water cooling
↓
Reduction of power consumption
Removal of mechanical support
↓
Shape rigidity of large-size, bent silicon wafers
Uniformly distributed material → no systematic error
See Valerio SARRITZU’s Pres.
Carbon foam spacers
27