## Slide 1: Significant performance recovery of SiPMs irradiation damage with in-situ current annealing
Xilei Sun
IHEP
Cape Town, 07/09 2023

## Slide 2: Contents
Motivation
Irradiation test
In-situ current annealing
Performance test
Summary

## Slide 3: Motivation
High Photon Detection Efficiency (PDE)
Fast Timing
Electromagnetic Field Insensitivity
High Voltage free
Compact Size
Array Configurations
Solid-State Robustness
Dark Count
Radiation damage effects
High Granularity Calorimeter
Space particle detection
Pros:
Cons:
SiPM-based detectors

## Slide 4: Compact Detectors for Microsatellite
Notes: Compact detector ideal for microsatellite

## Slide 5: On-orbit Irradiation Damage
Nuclear Inst. and Methods in Physics Research, A 1056 (2023) 168586

## Slide 6: Types and Effects of Radiation Damage
Increased Dark Current
Decreased PDE and Gain
Deteriorating Energy Resolution
Raised Detection Threshold
Displacement Damage
Ionization Damage
Types:
Effects :
lattice defects
Picture from the Internet

## Slide 7: Strategies to combat radiation damage
Radiation-Hardened Design
Protective Shielding
Operational Techniques
Calibration
Annealing
  off-line annealing
  In-situ Current Annealing
Picture from the Internet

## Slide 8: In-situ Current Annealing
No disassembly required
No External Heating Required
Passing a current through the SiPMs
Localized heating
Suitable for space applications and collider applications
T. Tsang et al 2016 JINST 11 P12002
M. Cordelli et al 2021 JINST 16 T12012
Picture from the Internet

## Slide 9: Experimental device - Irradiation Beam
Proton beam at China Institute of Atomic Energy (CIAE)
  with 5∼10 × 107 counts/cm2/s
Neutron beam at China Spallation Neutron Source (CSNS)
  6.9 × 106 counts/cm2/s

## Slide 10: Experimental device - SiPMs
Sensl MicroFJ-60035-TSV
Hamamatsu S14160-3010PS
NDL EQR15 11-3030D-S

## Slide 11: Experimental device – Annealing
Current source Keithley 2450
Thermal Camera Fluke TiS55+
Maximum T<260 ℃

## Slide 12: Experimental device – Performance test
Pico ammeter Keithley 6517
Cryogenic bins
LaBr3 scintillator crystal
Cs137 Excitation source
Data acquisition device 40 M/s

## Slide 13: Results- Temperature vs Current and Time
0.5A
0.6A
0.7A
0.8A
0.9A
(℃)
(s)
MicroFJ-60035-TSV
I

## Slide 14: Results- Dark Current vs Radiation
2 μA
0.03 μA
0.2 μA
Before
(860)
(180)
(405)

## Slide 15: Results- Dark current vs Annealing
2.7 × 108 n𝑒𝑞/cm2
2.7 × 109 n𝑒𝑞/cm2
4.6 × 1010 n𝑒𝑞/cm2
MicroFJ-60035-TSV
MicroFJ-60035-TSV
MicroFJ-60035-TSV
14%
10%
8%

## Slide 16: Results- Dark Current vs Annealing
1.0 × 1010 n𝑒𝑞/cm2
1.0 × 1012 n𝑒𝑞/cm2
1.0 × 1010 n𝑒𝑞/cm2
1.0 × 109 n𝑒𝑞/cm2
S14160-3010PS
S14160-3010PS
S14160-3010PS
EQR15 3030D SiPM
0.9%
1%
3%
6%

## Slide 17: Results- Dark Current vs Radiation and Annealing
Neutron Flux(n𝑒𝑞/cm2)
A: 2.7 × 108
B: 2.7 × 109
C: 4.6 × 1010
D: 1.0 × 109
E: 1.0 × 1010
F: 1.0 × 1012
G:1.0 × 1010

## Slide 18: Performance- Dark Current vs Temperature
Neutron Flux(n𝑒𝑞/cm2)
A: 2.7 × 108
B: 2.7 × 109
C: 4.6 × 1010
D: 1.0 × 109
E: 1.0 × 1010
F: 1.0 × 1012
G:1.0 × 1010

## Slide 19: Performance- Energy Resolution vs Temperature

## Slide 20: Performance- ADC vs Temperature
Fixed the operation voltage to 28.0 V

## Slide 21: Summary
Radiation damage effects is a major limitation for SiPMs
In-situ annealing with short time can significantly restore performance partially
Optional technology for Space and Collider applications
Nuclear Inst. and Methods in Physics Research, A 1053 (2023) 168381