## Slide 1: TID effects study on the monitoring system of the RD53 chip
Mohsine Menouni
On behalf of the RD53 collaboration
Aix Marseille University, CNRS/IN2P3, CPPM
Technology & Instrumentation in Particle Physics Conference TIPP2023
CTICC - Cape Town - South Africa – 4-8 September 2023

## Slide 2: Outline
Introduction
  RD53 project
  RD53 chip description
  Test results
Monitoring functions
  Description
  General Purpose ADC
  TID effects
RD53B sensors
  Temperature sensor principle
  Measurements based on the direct method
  Measurements based on the self-referencing method
  TID effects
Monitoring correction
Summary and Conclusion

## Slide 3: RD53 project
Characterization of the 65nm process in radiation
Several prototypes to qualify IP blocs (Analog FE, ADC, DAC, CDR/PLL, ShuntLDO …)
RD53A chip, Large-scale demonstrator with 3 FE flavors, Submitted in August 2017 and tested in an intensive way
ATLAS and CMS chips are two instances of the same common design, having different sizes and different Analog Front-End
RD53B chip (preproduction)
  ITkPix-V1 (ATLAS chip) submitted in March 2020
  CROC-V1 (CMS chip) submitted in May 2021
RD53C chip (Production)
  ITkPix-V2 (ATLAS chip) received in July 2023 and is still under tests and characterization
  CROC-V2 (CMS chip) to be submitted in September 2023
RD53 collaboration was established to design and develop pixel chips for ATLAS/CMS phase 2 upgrades
The RD53 project includes 24 institutes - ~20 designers
Extremely challenging requirements for HL-LHC
  Hit rates: 3 GHz/cm², Small pixels: 50 x 50 µm²
  Radiation: 500 Mrad - 1016 neq/cm² over 5 years
Technology: 65nm CMOS
ITkPix-V1 test board
RD53A
Size: 20 x 11.5 mm2
submitted in August 2017
RD53B-ATLAS (ITkPix-V1) size: 20 x 21 mm2
Submitted in March 2020
RD53B-CMS (CROC-V1) size: 21.6 x 18.6 mm2
Submitted in May 2021
RD53C-ATLAS (ITkPix-V2)
Submitted in March 2023
RD53C-CMS (CROC-V2) size: 21.6 x 18.6 mm2
To be submitted in Sept 2023

## Slide 4: RD53B Floorplan
Chip Bottom (Periphery)
  Analog Chip Bottom (ACB):
    Analog and mixed/signals building block for Bias, Calibration, Monitoring, and Clock/Data Recovery (CDR)
  Digital Chip Bottom (DCB):
    Synthesized digital logic
  Pad frame
    I/O blocks with ESD protections, ShuntLDO for serial powering
    Readout via serial links (1-4 x1.28Gbit/s) using Aurora64/66 encoding
Pixel array
  384 x 400 pixels of 50 x 50 µm²
  153 600 pixels organized in 2400 identical cores
  1 core  16 analog islands
  4 fronts ends per island
  Analog FE are embedded in a flat digital synthesized “sea”
  Time Over Threshold (ToT) digitization
  Shared Pixel Region buffer : Hit storage during Trigger latency
Pixel : 50 µm×50 µm
Core : 64 pixels
Chip Bottom

## Slide 5: RD53B-ATLAS test results
Before tuning:
Threshold: ~ 1860 e-
Thresh. dispersion: ~ 300 e-
Noise: 41 e-
After tuning:
Thresh. dispersion: ~ 80 e-
Noise: 40 e-
Threshold: ~ 700 e-

## Slide 6: Monitoring functions

## Slide 7: Monitoring description
The PAD “V_mux pad” is dedicated for optional external measurement
Monitored voltages (VMUX)
  Sensors, Calibration, FE, Reference voltages, Power supplies, and SLDO voltages
Monitored currents (IMUX)
  FE (Global DACs), CDR, CML, IREF, SLDO current
The IMUX output current is converted to voltage thanks to the external resistance R_IMUX and measured by selecting IMUX_OUT input in the VMUX
External NTC can be read out through the VMUX or the ADC
  It is supplied by a current from the I_NTC DAC (on-chip 10-bit DAC)
The on-chip 12-bit ADC is based on SAR architecture
The Integral Non-Linearity (INL) of the ADC is estimated to ±2 LSB
The Monitoring in the RD53 chip enables the digitization of several sensitive parameters in the chip :
  Voltages or currents in different parts of the chip
  Temperature
  Total ionizing dose
The Monitoring block contains :
  An analog current multiplexer (IMUX) followed by an analog voltage multiplexer (VMUX)
  A 12-bit Analog to Digital Converter (ADC)
IMUX
VMUX

## Slide 8: TID test results
Several TID test campaigns have been performed with X-ray sources at low temperatures (<-10 °C)
Measurements of the monitored voltages and currents as a function of the TID up to 650 Mrad were done with:
  External voltmeter at the VMUX_PAD and directly with the on-chip ADC
Example of the reference voltage VrefA that defines the value of power supply VDDA
Measurement Through the VMUX_PAD (Voltmeter)
  VrefA value is sensitive to the TID level
  At 500 Mrad: VrefA shift is +5%
VrefA (ADC) is different from VrefA (VMUX)
  The pre-irradiation value of VrefADC is used to convert the VrefA code, assuming that VrefADC is invariant with the TID
VrefADC is in fact sensitive to the TID and it shifts by +8% at 500 Mrad
If the variation of VrefADC with the TID is considered :
  VrefA (ADC) is very close to VrefA (VMUX)
VrefADC variation with the TID has the most significant impact on the measurement accuracy for the monitoring bloc
During the experiment runs, monitoring can be done only through the ADC. The VMUX out is not accessible at all
Find an entity in the chip with a very small variation with the TID that can be used as a reference for ADC measurements
This seems to be possible using some properties of the temperature sensor

## Slide 9: RD53B sensors

## Slide 10: RD53 temperature sensor
Different temperature sensors are implemented in the RD53B chip :
  Three active sensors are implemented in the chip bottom close to the shunt LDO circuit, considered the hottest part of the chip
    Based on NMOS diode-connected transistor
    Large area devices -> very tolerant to the TID effect
  Two sensors based on r-poly resistances are placed on the top and the bottom of the chip
    Monitor the temperature difference between the top and the bottom of the pixel array
  NTC device implemented outside the chip but the bias current is provided from the chip
The direct method for temperature measurement:
The two biases IBIAS and R×IBIAS are applied consecutively to the sensor
The temperature is calculated off-line based on the difference between DOUT2 and DOUT1
The potential sources of temperature measurement error:
  ADC non-linearity (INL -> ±1°C)
  The ratio R of the two sensor bias currents
  The Nf factor defining the weak-inversion slope
  VrefADC variation
Basic sensor structure

## Slide 11: RD53B temperature sensor
The mismatch of the ratio R of the current mirror can strongly reduce the measurement accuracy
  Dynamic Element Matching (DEM) is implemented to reduce this mismatch
    Interchanging the unit bias transistor using a switch array
    Up to 16 different values of ΔVD are measured and averaged
    Requires 32 ADC conversions to measure one temperature value
    Reduces significantly the error due to the ratio R
The weak-inversion slope factor Nf is sensitive to the process and the mismatch
  A calibration method was developed at ambient temperature and uses the external NTC to give the reference temperature
  Determine the Nf factor for each sensor with a high-precision
  Large area device used for the sensor makes Nf invariant with the TID
VrefADC is sensitive to the TID and the increase is 8% at 500 Mrad
  The temperature measurement variation with the TID is directly proportional to the variation of VrefADC
  A measurement error of about 20◦C at -10°C (263°K) can be reached at 500 Mrad Not acceptable
Dynamic Element Matching (DEM)

## Slide 12: Self-referencing method
The main purpose of this method is to avoid to include VrefADC for the temperature calculation
The new reference voltage is determined directly from the voltages across the sensor itself (VD and VD )
The absolute temperature is determined as :
A,  and VD(0) are process parameters
 represents the slope of VD (T), determined by measuring VD versus the temperature for each wafer batch process
VD(0) determined by extrapolating VD(T) for T=0K
A and  depends also on the sensor current  Needs chip-to-chip adjustment that can be done during the sensor calibration
The absolute temperature can be written as:
Temperature measurement depends directly on the DOUT2/DOUT1 ratio and so VrefADC is not considered in the calculation

## Slide 13: Measurement error
The drift of the bias current (IBIAS) with the TID is the principal cause of loss of precision in the temperature measurement
VD is not depending on the bias current (IBIAS)
VD increases with IBIAS and so VREF also increases
  The amount of VD increase is proportional to the absolute temperature Tab
If P denotes the relative change of IBIAS with the TID, VD shift is estimated to:
The table shows the drift of VD and of the temperature for P = 1% (50 Mrad) and P = 8% (500 Mrad)
The logarithmic variation of VD versus the IBIAS makes the relative variation of VD as well as the temperature less critical than that of the IBIAS
At 500 Mrad, the measurement error is less than 1◦C at -20 ◦C
This method remains largely more accurate since it is insensitive to VrefADC variation
The results look acceptable
Effects of IBIAS drift
TID effects on the temperature measurements
(50 Mrad)
(500 Mrad)

## Slide 14: ADC reference voltage correction

## Slide 15: Monitoring correction
All the reference voltages in the RD53B chip including VrefADC, are based on the reference current IREF generated from a band-gap circuit
IREF is sensitive to the TID  All the monitored voltages vary with the TID
VD = VD2 - VD1 related to the temperature sensor is insensitive to the current IREF and so it is insensitive to the TID if the temperature measurement is not shifting with the TID
The self-referencing method should be used during the experiment runs
VD can therefore be used as the reference voltage for the ADC
VD-rad voltage during the operation of the detector is calculated based on the pre-radiation value
The value of the effective LSB (LSBrad)of the ADC can thus be determined. (It corresponds to the VrefADC correction)
This LSBrad is then used to calculate directly the other voltages and current based on the output ADC codes
Adjusting some critical voltages can be applied if necessary

## Slide 16: Summary and conclusion
Radiation test campaigns have been performed with X-ray sources at low temperatures (<-10 °C)
  Variation of VrefADC with the TID -> increase by about 8% for 500 Mrad
  Temperature measurement using the direct method is not acceptable
A new method that does not use VrefADC is proposed and allows a good accuracy even for high TID levels.
Based on the two measurement methods of the temperature, a monitoring correction method is developed
It should respect the following steps :
Before the experiment runs:
  Calibrate temperature sensor chip by chip to compensate for the mismatch effect  Nf
  Determine process parameters for the temperature sensor : VD(0), α, and A
  Perform pre-irradiation measurements for each chip: VD_prerad and Tab_prerad , all the monitored Voltages, currents
During the experiment runs :
  The absolute temperature Tab-rad is measured with the self-referencing method
  The post-radiation VD_rad is determined knowing Tab-rad , VD_prerad and the corresponding Tab_prerad
  The LSB of the ADC (LSBrad) is then calculated and is used for the ADC code conversion
  Correction can be done at regular time intervals

## Slide 17: Thank you for your attention

## Slide 18: Monitored signals (Voltages)
Monitored signals : Sensors, Calibration voltages, FE, BG
SLDO voltages are monitored
Sensors : Temperature based on the voltage difference measurement
  Offset is compensated
Other Voltages : Variation from a starting value
  No need for ADC offset compensation
Value |  |  | Value | 
0 | VREF_ADC |  | 19-30 | NOT USED
1 | IMUX_OUT |  | 31 | VMON_VREF_CORE
2 | NTC |  | 32 | VMON_VREF_PRE
3 | VREF_VDAC |  | 33 | VMON_VINA
4 | VMON_HALFVDDA_INJCAP |  | 34 | VMON_VDDA
5 | RPOLYTSENS_TOP |  | 35 | VMON_VREFA
6 | RPOLYTSENS_BOTTOM |  | 36 | VMON_VOFS
7 | CAL_HI_GBL |  | 37 | VMON_VIND
8 | CAL_MI_GBL |  | 38 | VMON_VDDD
9 | VTH2G |  | 39 | VMON_VREFD
10 | VTH1G_M |  |  | 
11 | VTH1G_L |  |  | 
12 | VTH1G_R |  |  | 
13 | RADSENS_SLDOA |  |  | 
14 | TEMPSENS_SLDOA |  |  | 
15 | RADSENS_SLDOD |  |  | 
16 | TEMPSENS_SLDOD |  |  | 
17 | RADSENS_ACB |  |  | 
18 | TEMPSENS_ACB |  |  | 

## Slide 19: Monitored signals (Currents)
Select the IMUX_OUT channel of the voltage multiplexer
IREF, FE (Global DACs), CDR, CML, NTC
New features in RD53B :
  The external NTC will be read through the ADC
    The NTC current bias is provided inside the chip
  SLDO currents are monitored
Value |  |  | Value | 
0 | MON_IREF |  | 16 | MON_TH1_M
1 | MON_VCO_CDR |  | 17 | MON_LCC
2 | MON_VCOBUFF_CDR |  | 18 | MON_VFF
3 | MON_CP_CDR |  | 19 | MON_PREAMP_L
4 | MON_CP_FD_CDR |  | 20 | MON_TH1_L
5 | MON_CP_BUFF_CDR |  | 21 | MON_PREAMP_R
6 | MON_CML_BIAS_2 |  | 22 | MON_PREAMP_TL
7 | MON_CML_BIAS_1 |  | 23 | MON_TH1_R
8 | MON_CML_BIAS_0 |  | 24 | MON_PREAMP_T
9 | MON_BIAS_NTC |  | 25 | MON_PREAMP_TR
10 | MON_INJCAP |  | 26 | NOT USED
11 | MON_INJCAP_PAR |  | 27 | NOT USED
12 | MON_PREAMP_M |  | 28 | MON_IINA
13 | MON_PRECOMP |  | 29 | MON_ISHUNTA
14 | MON_COMP |  | 30 | MON_IIND
15 | MON_TH2 |  | 31 | MON_ISHUNTD

## Slide 20: General Purpose 12-bit ADC
The ADC main clock is set to 39 kHz (40 MHz/1024)
The ADC tests and characterization were done with commercial 16-bit DACs (LSB is 27.5μV)
For a reference voltage of 900 mV, the LSB value is 208 μV and related to the VrefADC value by :
The factor 0.947 takes into account the effect of the load capacitance seen at DAC on the output
The peak INL is estimated to be ±2 LSB and the plot shows that the INL has a jump at the middle of output codes
The 12-bit ADC is based on a Successive-Approximation Register (SAR) architecture and consists of 3 main circuits
  A 12-bit DAC based on a capacitance network
  A high-sensitivity comparator
  A SAR logic block

## Slide 21: General Purpose 12-bit ADC
The 12-bit ADC is based on a Successive-Approximation Register (SAR) architecture
The circuit takes the chip bunch crossing clock, nominally 40 MHz, and divides it down with a 1024:1 frequency divider to generate the internal clock driving the ADC at 39 kHz
The SAR ADC consists of three main circuits (Fig. 2):
  A 12-bit DAC based on a capacitance network supplied through the reference voltage (VrefADC) to generate the voltage scaling
  A high-sensitivity comparator
  A SAR logic block including the frequency divider mentioned above

## Slide 22: TID effects on temperature sensors
measured at the MUX output :
  The measured temperature increases from a TID of 300 Mrad
  This is in agreement with the temperature given by the NTC
  The increase is mainly due to the increase of the analog power consumption
VREF_ADC increases by ~ 8% during TID tests
  Compatible with measurements done by other institutes
  Without calibration of the ADC reference voltage :
    the temperature, measurement error is estimated to ~3°C each 1%
    Measurement error = +20°C for 8% (500Mrad)
more accurate temperature measurement method is needed
  Not dependent on the ADC reference voltage

## Slide 23: Global calibration with the NTC
The global calibration consists in defining the ideality factor Nf to be used by default for all the 4 sensors
This calibration is based on the voltage measured at the output PADs (The ADC is not yet used)
Measurements with climate chamber done for the different RD53A configurations
  Default : Default configuration BDAQ software
  Low Analog Power : Switch off all the analog pixel bias currents
  Low global power : Switch off all the pixel bias currents and disable the pixel array clock
  High current: Default configuration + Shunt mode setting
For the power off : Temp-TS = Temp-TNC
Adjust the ideality factor Nf regarding the NTC temperature
  Default Power : Temp-TS = Temp-TNC + 3°C @ ~25°C
  Low Power : Temp-TS = Temp-TNC + 1°C @ ~25°C
For the RD53A, the default ideality factor for the sensor
  BJT: Nf = 1.008
  NMOS : Nf = 1.225
 | Default | Low Analog Power | Low global power | High power
IDIG | 450 mA | 444 mA | 130 mA | 1166 mA
IANA | 300 mA | 71 mA | 55 mA | 1087 mA

## Slide 24: Mismatch in the same chip
Measurements done for Direct Powering
  Default power : 974 mW (Ivdda= 392 mA Ivddd=362 mA)
Default ideality factor :
  BJT: Nf = 1.008
  NMOS : Nf = 1.225
Small effect of the mismatch inside the same chip
For T>30°C Temp(TS) is higher than expected (+3°C at 50°C)
  The power Increase with the temperature can explain a part of this error

## Slide 25: TS Mismatch effect and calibration
10 chips were tested from -40°C to 50°C using climatic chamber
Statistics on 6 chips biased in direct powering with applying the same parameter Nf=1.255 (default settings)
Calibration chip by chip is required
  Define the ideality factor Nf
  Only one measurement point is required
  Use direct powering
  Adjust Nf regarding the NTC temperature
    Default Power : Temp-TS = Temp-TNC + 3°C @ ~25°C
    Low Power : Temp-TS = Temp-TNC + 1°C @ ~25°C

## Slide 26: Temperature calculation
 is a constant
  Used as a mapping coefficient between non linear and linear
  Used for trimming purpose
VD/VD
=.VD/(VD+. VD)

## Slide 27: NMOS Temperature Sensor
Less damage than the BJT
Very small shift in the characteristics
NMOS : W/L = 20/1*32

## Slide 28: Monitoring calibration
During the detector production period
  Use VD = VD2-VD1 for the temperature measurement
  Measurements based on external precise voltmeter
  Calibration is mandatory
During the detector exploitation period
  Use the ratio DOUT2/DOUT1 for the temperature measurement
  A and  are process parameters
   needs to be adjusted taking into account the Nf factor variation (chip to chip)
During the detector exploitation period
  VD voltage is insensitive to the IREF and insensitive to the TID. It is also insensitive to the power supply variation
  Depends on the temperature that can be measured with a good precision
Consider VD as a reference voltage for monitoring and calibration

## Slide 29: Monitoring correction
The effective VD voltage during the operation of the detector is calculated as :
The value of the effective LSB of the ADC can thus be determined by:
    Where :
This LSBeff is then used to calculate directly the other voltages and current values based the output ADC codes
Adjusting some critical voltages can be applied if necessary
All the reference voltages in the RD53B chip including VrefADC, are based on a copy of the reference current IREF generated from a band-gap circuit
IREF is sensitive to the TID  All the monitored voltages vary with the TID
VD = VD2-VD1 measured across the temperature sensor is insensitive to the current IREF and so insensitive to the TID
But VD depends on the temperature of the chip
Temperature measurement with good accuracy is needed and this can be done with the self-referencing method :
VD can therefore be used as the reference voltage for the ADC