## Slide 1: Heat Dissipation Improvement of ATLAS Electronics by Thermal Interface Materials Based on Carbon Nanomaterials
Department of Physics
Presented by: Othmane Mouane

## Slide 2
ATLAS / TileCal
Particle detectors of the LHC accelerator had been designed to have integrated electronics.
big constraints: continuous radiation exposure, very limited space, only water cooling available, and an external DC magnetic field from superconducting magnets.
Protecting the electronics inside the detectors from damages and overheating, and expanding their lifespan, is required.
Continuous and good heat dissipation is necessary.
Low Voltage Power Supply (LVPS)
The LVPS brick is a 6 layer board with dimensions 80.26 mm square.
The main electronic components are the transformer, MOSFETs and inductors.
The thermal posts are in contact with the rear of the electronic components via a third-party material referred as the Thermal Interface Material (TIM).
MOSFET
T2
Inductor
×
×
×
×
×
×
MOSFET
Thermal Interface Materials (TIM)
Material utilised in between two interfaces in electronic devices.
TIM are polymer or metal-based materials, filled with conductive particles.
Protect expensive systems (overheating, damage…), expand their lifespan.
Heat conduction coefficient of the Thermal Interface Material is considered low for many contemporary applications (micro- and nano-electronic…).
Integrating Carbonaceous Nanomaterials
1
Part of the upgrade of TileCal
Improve reliability through redundancy to limit the impact of component failures.
All electronics to be replaced with newer technologies and should be radiation hard.

## Slide 3: Carbon Nanomaterials
Global Nanotechnology Market & Forecast to 2024
The global nanotechnology market is expected to exceed US$ 125 Billion mark by 2024.
the nanomaterials captured highest share of the global nanotechnology market.
Nanoparticles holds over 85% share of the global nanomaterials market.
Carbon Allotropes
3D: Graphite, Diamond, Amorphous Carbon.
2D: Graphene, Carbon nanoribbons (unzipped carbon nanotubes).
1D: Carbon Nanotubes (single and multi walled), Carbon Nanohorns.
0D: Fullerene, Nanodiamonds, Carbon Dots, Carbon Nanospheres.
Applications
Electronics, Energy, Biomedicine, as controlled/targeted drug delivery systems, supercapacitors, catalyst supports, superconductivity, hydrogen storage1.
1 "A. A. Deshmukh, S. D. Mhlanga and N. J. Coville, "Carbon spheres," Materials Science and Engineering: R: Reports, vol. 70, no. 1-2, pp. 1-28, 2010.
2

## Slide 4: Preparation of TIM (Epoxy/CNMs)
Furnace
Quartz tube
Gas input
Gas output
600-1200 °C
Carbon nanomaterials
Hydrocarbon gas
Seal
3

## Slide 5: Experimental Setup
Q  ΔT
ΔT = Tin – Tout
Q  1/Tout
Q : Heat transfer
ΔT : Temperature gradient
Tout : Temperature of the post
4

## Slide 6: Results (TIMwith-CNTs vs TIMwithout-CNTs)
Q0.5% of CNTs > QEpoxy
Q0.7% of CNTs > QEpoxy
Q1% of CNTs > QEpoxy
Q3% of CNTs > QEpoxy
Q5% of CNTs > QEpoxy
Q10% of CNTs < QEpoxy
Q1% of CNTs > Q5% of CNTs > Q0.5% of CNTs > Qepoxy > Q10% of CNTs
5

## Slide 7: Results (TIMwith-CNSs vs TIMwithout-CNSs)
6
Q0.5% of CNSs > QEpoxy
Q1% of CNSs > QEpoxy
Q5% of CNSs > QEpoxy
Q1% of CNSs > Q0.5% of CNSs > Q5% of CNSs > Qepoxy
Amount of CNM (%) | Tdiff of TIMCNTs (°C) | Tdiff of TIMCNSs (°C)
0.5 | 1.33 ± 0.05 | 1.45 ± 0.04
0.7 | 1.87 ± 0.03 | -
1 | 2.0 ± 0.1 | 1.64 ± 0.04
3 | 1.69 ± 0.07 | -
5 | 1.38 ± 0.1 | 1.12 ± 0.11
10 | (-)1.08 ± 0.07 | -
Amount of CNM (%) | Tdiff of TIMCNTs (°C) | Tdiff of TIMCNSs (°C)
0.5 | 1.33 ± 0.05 | 1.45 ± 0.04
0.7 | 1.87 ± 0.03 | -
1 | 2.0 ± 0.1 | 1.64 ± 0.04
3 | 1.69 ± 0.07 | -
5 | 1.38 ± 0.1 | 1.12 ± 0.11
10 | (-)1.08 ± 0.07 | -
The magnitude of the gap between the temperatures of the two posts depends on the amount of carbon nanomaterials incorporated.
Incorporation of carbon nanomaterials in the thermal compound results in a heat conduction enhancement.
The heat transfer of TIMs with 1% of CNTs is observed to be larger in comparison to TIMs with 1% of CNSs.
The gradual decrease in the heat transfer for TIMs containing more than 1% of carbon nanomaterials is due the CNT-CNT or CNS-CNS couplings.
Clear and desirable adhesive contact was observed while trying to dismount the Al2O3 posts from the heat source.
The temperature gradient tdiff as a function of the amount of the carbon nanomaterials incorporated in the TIMs
The recorded temperatures over 24 h for TIMs with 0% and 0.5% of CNSs and CNTs. The measurements show the consistency of the temperature gradient Tdiff at the steady state over time in hours.
The temperature gradient Tdiff (filled markers) and the repeated measurements (empty markers) plotted as a function of the amount of CNTs and CNSs. The graphs show the reproducibility and sustainability of the temperature gradient over time.

## Slide 8: Thermal resistance characterization (ASTM D5470 approach)
The thermal resistance Rth of the TIM with 1% of CNTs was estimated to be 80.14 mm2K/W, while for TIM with 1% of CNSs, it was calculated to be 100.9 mm2K/W.
The measured thermal resistance of the fabricated TIMs shows a significant upgrade in the thermal properties of the initially used heat transfer compound (Unick) as a base (50 % decrease).
Rth= 100.90 mm2K/W
Rth= 80.14 mm2K/W
7
TIM | RTh (mm2K/W)
Unick | 200
ZS-GF-Z10 | 150
TG-AS606B | 94.73
RS S606C | 36
The thermal resistance Rth of various TIMs with a thickness of 180 μm.

## Slide 9: Applicability on test bench and burn-in station
TIM only
TIM with 1% of CNTs
8
The incorporation of 1% of CNTs in the thermal compound shows a temperature drop of 6.5 °C (30.48 to 23.9 °C) for T2, while a decrease of 9.2 °C (27.34 to 18.08 °C) is depicted for temperature T3
Temperatures T2 and T3 of the brick tested in the burn-in station with TIMs containing 0% (dashed) and 1% (continuous) of CNTs separately with identical parameters.
The plots reveal a large decrease of temperatures of the brick operating with 1% of CNTs based TIM.

## Slide 10: Summary
As part of the upgrade of the Atlas detector a continuous and high heat dissipation within the electronic devices is required for a good performance.
Integrating Carbon nanomaterials in the thermal interface materials.
The integration of carbon nanomaterials in the epoxy showed an important enhancement of the heat dissipation in comparison to the use of only the commercial epoxy.
The improvement is measured to reach 2 °C with a 1% of Carbon Nanotubes and 1.6 °C with 1% of Carbon Nanospheres.
The measured thermal resistance of TIMs containing 1% of CNTs (80.14 mm2K/W ) and 1% CNSs (100.90 mm2K/W ) were in accordance with the measurements recorded by the test stand.
This innovation in the fabrication of TIMs based on carbon nanomaterials is important for electronic devices in general as well as for the LVPS bricks in particular as it protects against overheating and damage and ensures a longer life span
9

## Slide 11: Thank you