## Slide 1
Mechanical stresses in solids irradiated with swift heavy ions: in-situ and post-radiation examination
Vladimir Skuratov
Flerov Laboratory of Nuclear Reactions
Joint Institute for Nuclear Research
Dubna, Russia

## Slide 2
Main questions addressed to real-time measurements:
Radiation damage and stress accumulation processes before and
after ion track region overlapping
Variation in the stress state under ion irradiation characterized
by specific ionizing energy losses higher and lower than the threshold
of radiation damage formation via electronic excitations.
Motivation
The knowledge about of high energy (E> 1 MeV/amu) heavy ion-induced stress is of considerable practical value in view of simulation of fission product impact in radiation resistant oxides and ceramics, considered as candidate materials for nuclear waste management (inert matrix fuel host)
Notes: Radiation defects produced by swift heavy ions are concentrated within small volume, surrounding ion trajectory. This inevitably results in generation of local mechanical stress, which in own turn may affect final defect structure. The knowledge about of such a high energy heavy ion track-assisted stress is of considerable practical value in view of simulation of fission product impact in radiation resistant oxides and ceramics, as candidate materials for nuclear waste management and prediction of their long-term radiation stability. In this report we give a review of experiments aimed at evaluation of mechanical stresses in radiation resistant ceramics (Al2O3, Si3N4, AlN) during and after irradiation with high energy Kr, Xe and Bi ions. To characterize stress a piezospectroscopic method, utilizing the relationship between the stress and changes in the ionoluminescence, photoluminescence and Raman spectra has been used.

## Slide 3
Experimental techniques which can be used used for evaluation of
mechanical stress accumulation during ion irradiation
X-ray diffraction
Motivation

## Slide 4
Accumulation of mechanical stresses under swift heavy ion irradiation
XRD is not convenient for real-time examination
Notes: The d-spacing can described as the distance between planes of atoms that give rise to diffraction peaks. Each peak in a diffractogram results from a corresponding d-spacing. The planes of atoms can be referred to a 3D coordinate system and so can be described as a direction within the crystal. So d-spacing as well as having a dimension, usually quoted in Ångstroms, can labelled with a plane direction hkl.

## Slide 5
Experimental techniques which can be used used for evaluation of
mechanical stress accumulation during ion irradiation
X-ray diffraction
Optical piezospectroscopy
Piezospectroscopic effect connects the changes in optical spectra (absorption, luminescence, Raman) with changes in stress state of material
Motivation

## Slide 6
Basis of the piezospectroscopic effect – the applied stress strains the lattice and alters the energy of transitions between electronic states
 = ij×ij
ij – piezospectroscopic coefficients
Typical piezospectroscopic probes: Cr3+ in Al2O3
Eu3+, Nd3+ in silica glasses
Sm3+ in borosilicate glasses
R1-line
R2-line
D. Clarke et. al.
Accumulation of mechanical stresses under swift heavy ion irradiation

## Slide 7
Dose dependence of ionoluminescence spectra in Al2O3:Cr measured
during 167 MeV Xe ion irradiation at 80 K.
Accumulation of mechanical stresses under swift heavy ion irradiation

## Slide 8
Ion fluence, cm-2
wavenumber, cm-1
Kr
Xe
Se=25 keV/nm
Se=16 keV/nm
The stresses are compressive in basal plane of the sample and tensile in perpendicular direction
each Cr3+ ion acts as an independent strain sensor
The splitting of the R-lines directly indicates on the presence of differently stressed regions in the irradiating ruby specimen
Accumulation of mechanical stresses under swift heavy ion irradiation

## Slide 9
wavenumber, cm-1
Ion fluence, cm-2
Xe
Se=25 keV/nm
Accumulation of mechanical stresses under swift heavy ion irradiation

## Slide 10
167 MeV xenon ion induced tracks in Al2O3

## Slide 11
J.H. O’Connell et al., NIM B (2015), http://dx.doi.org/10.1016/j.nimb.2015.09.067
Normalized density variation as a function of radial distance from the track center (MD simulation)
Two experimental plots of 1 mean basal plane lattice dilation as a function of radial distance from the track center (TEM images processing)

## Slide 12
Kluth et al. J. Appl. Phys. 110, 123520 (2011)
Density profiles of 185 MeV Au ions fit for α-SiO2 irradiated to a fluence of 6×1012 ions/cm-2.

## Slide 13
σh
R
STRESS IN Al2O3:Cr UNDER SWIFT HEAVY ION IRRADIATION
R1 = 2.9 nm
R2 = 5.2 nm
R2
R1
167 MeV Xe

## Slide 14
STRESS IN Al2O3:Cr UNDER SWIFT HEAVY ION IRRADIATION
1=3.26(11+22)+1.5333
2=2.73(11+22)+2.1633
ii (i = 1, 2, 3) – stress tensor components, oriented along a, m and с axes
Bi,700 MeV
Xe,167 MeV
Kr,107 MeV

## Slide 15
STRESS IN Al2O3:Cr UNDER SWIFT HEAVY ION IRRADIATION

## Slide 16
1 =3.26(11+22)+1.5333
2=2.73(11+22)+2.1633
ii (i = 1, 2, 3) – stress tensor components, oriented along a, m and с axes
Depth variation of the R-lines luminescence spectra in 107 MeV Kr and 167 MeV Xe ion irradiated ruby crystals
Stress profiles in swift heavy ion irradiated Al2O3:Cr single crystals

## Slide 17
Depth variation of the R-lines luminescence spectra
in 670 MeV Bi ion irradiated ruby crystals
Stress profiles in swift heavy ion irradiated Al2O3:Cr single crystals

## Slide 18
Residual stress and ionizing energy loss profiles in Al2O3:Cr
h (GPa)  2(cm-1)/7.61 Rp=21 m

## Slide 19
Mechanical stress profiles in radiation-resistant ceramics irradiated with high-energy heavy ions: Si3N4 vs AlN
Silicon and aluminium nitrides have different structural response to swift heavy irradiation
The threshold of amorphous latent track formation in Si3N4 = 17 keV/nm
No latent tracks are registered in AlN till (dE/dx)ion < 35 keV/nm

## Slide 20
Si3N4 + Bi 710 МэВ

## Slide 21: p-Si3N4 + Xe 220 МэВ, 2х1014 см-2

## Slide 22: p-Si3N4 + Bi 710 МэВ, 1,2x1013 см-2

## Slide 23
Mechanical stress profiles in Si3N4 and AlN irradiated with swift heavy ions: microraman piezospectroscopy examination
Si3N4 ij = 2.22 cm-1/GPa
ij – piezospecroscopic coefficients
 = ij×ij
Depth resolution = 1 мкм
 = 862 cm-1
AlN4 ij = 2.0 cm-1/GPa
 = 658 cm-1

## Slide 24
Профили механических напряжений в Si3N4, облученном ионами ксенона и висмута: Анализ методами микрорамановской пьезоспектроскопии
 = 862 cm-1

## Slide 25
AlN + Bi 710 МэВ

## Slide 26
Depth profiles of mechanical stresses Si3N4, irradiated with swift Bi and Xe ions: Depth-resolved microraman examination

## Slide 27
Schematic drawing of SHI irradiated target and energy loss profiles

## Slide 28
Cross-sectional SEM image of Si3N4 irradiated with 167 Xe ions
Si3N4 + Xe 167 МэВ

## Slide 29
Variation of the spectral position of the 862 cm-1 (Si3N4) and 658 cm-1 (AlN) lines with the Bi ion fluence over the depth of the irradiated layer

## Slide 30
Thank you for your attention!